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	Reference.
0205. Glove PE
COD. GTIN/EAN13
Bag 100 units: 8436036491333
Use
To avoid contamination of the products handled, as well as to protect the user's hands from soiling.
Preferential use in supermarkets and department stores (self-service greengrocers and frozen foods).
At service stations to avoid direct contact with lubricants.
Storage gloves: The product will maintain its properties as long as it is stored in dry places, at a temperature between 10ºC and 30ºC. Do not expose to direct light. Five years expiration
Regulation
Royal Decree 866/2008, on plastic materials intended to come into contact with food, which transposes Directive 2002/72 / EC (update by European Regulation 10/2011)
Global migration test according to the UNE-EN 1186: 2002 Standard.
Minimal Risk Cat I. Regulation EU 2016/425
	
	Characteristics
· High Density  (HDPE) transparente.
· Slightly embossed.
· One size
· Food contact
· CE marking
Lenght glove: 300 mm
Cuff glove: 70mm
Palm: 140mm
thickness: 0’01mm

Measures
Box: 32x21x24cm
Weight per box: 6.3kg
Format
Bag: 100 units
Box 100 bags.
100 x 100: 10.000 units box
Pallet: 64 ctn. 640.000 bags.
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